Supporting Information

Figure S1. The SEM spectra of (a-c) Mo2C, (d-f) Mo₂C-MoC/NC-0.1, (g-i) Mo₂C-MoC/NC-0.5.

Figure S2. The corresponding elemental maps of C, N, O, and Mo of the Mo2C-MoC/NC-0.3 catalyst sample.

Table S1. The corresponding elemental table of C, N, O and Mo in the Mo2C-MoC/NC-0.3 catalyst sample.

| Element (keV) | Mass% | Atom% | Sigma |
| --- | --- | --- | --- |
| C K N K O K Mo L (Ref.) | 0.42 0.21 2.14 97.24 | 2.92 1.23 11.17 84.68 | 0.04 0.03 0.08 0.86 |

Figure S3. The CV of (a) Mo2C-MoC/NC-0.1, (b) Mo2C-MoC/NC-0.3, (c) Mo2C-MoC/NC-0.5, (d) Mo2C, (e) 20% Pt/C, with the scan rates of 20, 40, 60, 80, 100, 120 and 140 mV·s-1 in 1.0 M KOH.

Figure S4. (a) ECSA values of various catalysts, (b) ECSA-normalized LSV curves of different catalysts for HER.

Figure S5. The LSV curves before and after 1000 cycles of CV test in 1.0 M KOH.

Figure S6. (a) SEM, (b,) TEM, (c-e) HRTEM of Mo2C-MoC/NC-0.3 after long-term cycling experiments.

Figure S7. The XPS spectra of Mo2C-MoC/NC-0.3 after long-term cycling experiments (a) The XPS spectra of C 1s in Mo2C-MoC/NC-0.3. The test results indicate that the sample still contains elements such as Mo, C, and O. In addition, there are also small amounts of elements with F and K. The C-F and C-K bonds in the figure confirm their existence, which may be due to the attachment of K+ ions in the alkaline electrolyte, and the experiment used Nafion solution containing F elements, resulting in the retention of some elements. (b) The XPS spectra of Mo 3d in Mo2C-MoC/NC-0.3.

Table S2. Comparison of η10 for Mo₂C-MoC/NC-0.3 with the recently reported Mo2C-based HER electrocatalysts.

| Sample | η10 (mV) | Tafel (mV dec-1) | Reference |
| --- | --- | --- | --- |
| Mo2CeMoC/NF-650 | 28.6 | 73 | [1] |
| ZNDM-MoC/Mo2C | 69 | 57.9 | [2] |
| Fe-Mo2C @ NCF | 76 | 65 | [3] |
| Mo2C/Mo3N2/C | 76 | 52.6 | [4] |
| Mo2C/MoC/MoP@NC-650-0 | 78 | 52 | [5] |
| Co/MoC@NC | 80.6 | 128 | [6] |
| Mo2C/MoC/CNT | 82 | 42 | [7] |
| NiCo-MoxC | 86.6 | 62.8 | [8] |
| Mo2C-MoC/NC-0.3 | 87 | 54.8 | this work |
| MoO2/MoC | 104 | 60.0 | [9] |
| B-Mo/Mo2C | 108 | 52.7 | [10] |
| Mg-Mo2C | 111 | 68.23 | [11] |
| Mo2C/MoC-1 | 119 | 49.8 | [12] |
| Zn-MoC/Mo2C | 139 | 50 | [13] |
| Mo2C-MoC/C | 139.4 | 55 | [14] |
| P-Ni-Mo2C-2h | 140.5 | 50.7 | [15] |
| Ni0.5@MoCx/NC | 150 | 74.6 | [16] |
| W-MoxC/C | 178 | 54.3 | [17] |
| β-Mo2C/α-MoC1-x | 242 | 78 | [18] |
| Co-MoxN/Mo2C | 297 | 120.7 | [19] |